## Slide 1
D u k e
U N I V E R S I T Y
614-600-6861
Erica.babusci@duke.edu
Testing the Efficacy of Micro-Blaze Detergent on PAH Removal from Firefighter Uniforms
Erica Babusci1, Claudia K. Gunsch1, and Heather Stapleton2
Department of Civil and Environmental Engineering, Duke University
Nicholas School of the Environment, Duke University
A
Background
This material is based upon work supported by the National Institute of Environmental Health Sciences Under Grant No. P42ES010356
Methods
References and Acknowledgements
Future Directions
Results For Micro-Blaze Treatment
Sample Preparation
A section from the arm of a firefighter jacket was provided from the Stapleton lab. Samples of 1 cm by 1 cm were cut and used for each experimental group in triplicate.
Treatments
Cuttings were exposed to one of the following wash treatments:
Control (no treatment)
5% Micro-Blaze3
5% Tide
Tap water
Wash steps involved 10 mL of wash liquid in a 50 mL beaker and left at room temperature on a plate shaker at 100 rpm for 1 hour.
Data Acquisition
Samples were then air-dried and packaged to be returned to the Stapleton lab for PAH extraction and GC-MS analysis.
[1] Kim et al. (2013) Environment International [2] Baxter et al. (2014) J Occup Environ Hyg [3] Verde Environmental, Inc (2025) Micro-Blaze Products [4] Seo, J.-S., Keum, Y.-S., & Li, Q. X. (2009). Bacterial Degradation of Aromatic Compounds.
Figure 4: Experimental groups tested for the study
Objectives
s
Evaluate the effectiveness of Micro-Blaze treatment compared to tap water and standard detergents in removing PAHs from firefighter gear.
Polycyclic aromatic hydrocarbons (PAHs) are a group of harmful chemicals that have carcinogenic and mutagenic properties.1,2,4 These compounds are formed through the partial combustion of organic material and accumulate on firefighter PPE, leading to long-term exposure and posing serious health effects.1 Micro-Blaze PPE DE-CON Cleaner (MB) is a product marketed as a spore-containing detergent that not only removes the PAHs but degrades them into nontoxic byproducts.3
Analyze PAH extractions of the wash water to determine if compounds are being degraded or emulsified
Figure 2: Micro-Blaze PPE DE-CON cleaner
This project aims to investigate the efficacy of this product for decontaminating firefighter PPE. Using cuttings from a used firefighter jacket and different treatment types, the project investigates the efficacy of using Micro-Blaze DE-CON cleaner to remove and degrade PAHs from the firefighter jacket.
Figure 7: Experimental design for future work exploring PAH removal pathways.
Figure 1: Overview of PAH exposure and effect on PAHs
Figure 3: Schematic of firefighter cuttings
Figure 5 (A-B): Figures depict the chemical composition of the PAHs and how the chemical properties of different PAHs affect removal efficiencies. A: Bar plot looking at relative abundance of each PAH on the control jacket. B: Scatterplot depicting how the percent removal of each PAH is correlated to their respective log Kow. Percent removal is calculated by dividing the Micro-Blaze concentrations to the control/unwashed concentrations
Figure 6 (A-C): Figures are depicting the different in mean PAH concentration between treatment groups. A looks at Phenanthrene (4 rings), B looks at Benzo[j,b,k]fluoranthene (5-rings), and C looks at Fluoranthene (6-rings). Shapiro Wilks test was used to test normality. Fluoranthene was determined to be non-parametric, and a Kruskal-Wallis test was used to test significance. ANOVAs were used for Benzo[j,b,k} fluoranthene and Phenanthrene. Groups with p values < 0.05 were determined to be significant. This trend was seen for 14/16 PAHs
A
B
b
c
a
a
a
A
B
C